TiO2 nanotubes modified with cadmium oxide for photoelectrocatalytic oxidation of alcohols

Vitali Grinberg ˑ Victor Emets ˑ Alexey  Shapagin ˑ Aleksey  Averin ˑ Andrei Shiryaev

Frumkin Institute of Physical Chemistry and Electrochemistry, Russian Academy of Sciences, Leninsky Prospekt 31, Building 4, 119071 Moscow, Russia

* Correspondence: victoremets@mail.ru; Tel.:  +7(495) 955-40-23

Supplementary materials

0.05 C

ZAF Method Standardless Quantitative Analysis

Fitting Coefficient : 0.2626

Element        (keV)   mass%  Error%     At%  Compound   mass%  Cation         K

C K           0.277    1.97    0.05    4.73                              1.2149

O K           0.525   30.27    0.47   54.57                             12.6515

Ti K           4.508   67.46    0.34   40.63                             85.7918

Cd L*          3.132    0.30    0.47    0.08                              0.3418

Total                 100.00          100.00

ZAF Method Standardless Quantitative Analysis

Fitting Coefficient : 0.2679

Element        (keV)   mass%  Error%     At%  Compound   mass%  Cation         K

C K           0.277    2.17    0.05    5.02                              1.3691

O K           0.525   33.10    0.43   57.51                             14.6929

Ti K           4.508   64.45    0.33   37.40                             83.6111

Cd L*          3.132    0.28    0.46    0.07                              0.3269

Total                 100.00          100.00

0.2 C

ZAF Method Standardless Quantitative Analysis

Fitting Coefficient : 0.2617

Element        (keV)   mass%  Error%     At%  Compound   mass%  Cation         K

C K           0.277    1.62    0.05    3.91                              1.0134

O K           0.525   30.89    0.45   55.88                             13.1659

Ti K           4.508   65.86    0.33   39.79                             83.9665

Cd L           3.132    1.62    0.46    0.42                              1.8542

Total                 100.00          100.00

1/1

0.8 С

1/1

1/1

Fig. S1. Duration of the first and second anodization step – 60 min followed by cathodic deposition of varying amounts of cadmium oxide 0,05, 0,2 and 0,8 C correspondingly and Standardless Quantitative Analysis.

(a)

(b)                                                                                  (c)

(d)

| Peak name |  | Eb, eV | Quant., at.% |  |
| --- | --- | --- | --- | --- |
| Ti2p | TiO2 | 459 | 25,95 | 25,95 |
| Cd3d | Cd | 405,6 | 0,12 | 0,12 |
| O1s | H2O | 533 | 3,36 | 73,93 |
|  | C-O | 531,8 | 10,81 |  |
|  | C=O | 531 | 7,9 |  |
|  | TiO2 | 530,2 | 51,86 |  |

Fig. S2. XPS spectra of cadmium-modified TiO2-NTbs prepared by cathodic deposition of CdО (0.2 C/cm2) (a) High-resolution XPS spectra of Ti 2p, Cd 3d and O 1s(b-d). The sample was calcined at 450 °C in air for 1 h.

Fig. S3. TEM image of the supermolecular surface structure of  TNT – (0.2)CdO.

Fig. S4. Wavelength dependence of IPCE% for the TNT and TNT–(0.05)CdO photoanodes in 0.1 M Na2SO4 aqueous solution.