Electronic supplementary materials

SYNTHESIS, STRUCTURE AND NONCOVALENT INTERACTIONS OF MESITYL(PHENYL)PHOSPHINE OXIDE GLYCOLATE BASED HYDROGEN-BONDED NANOSIZED ORGANIC FRAMEWORK

A.A. Kagilev1, I.F. Sakhapov1, Z.N. Gafurov1, A.O. Kantyukov1,2, I.K. Mikhailov1, D.R. Islamov3, A.V. Gerasimov2, O.A. Filippov4, A.T. Gubaidullin1, O.S. Soficheva1, O.G. Sinayshin1, D.G. Yakhvarov1,2,*

1Arbuzov Institute of Organic and Physical Chemistry, FRC Kazan Scientific Center, Russian Academy of Sciences, 420088, Kazan, Russian Federation

2A.M. Butlerov Institute of Chemistry, Kazan Federal University, 420008, Kazan, Russian Federation

3Laboratory for Structural Studies of Biomacromolecules, FRC Kazan Scientific Center, Russian Academy of Sciences, 420111, Kazan, Russian Federation

4A.N. Nesmeyanov Institute of Organoelement Compounds, Russian Academy of Sciences, 119991, Moscow, Russian Federation

yakhvar@iopc.ru

Table S1 Crystallographic data of mesityl(phenyl)phosphine oxide glycolate 1

| Compound | 1 |  |
| --- | --- | --- |
| Formula | C17H19O4P |  |
| Formula weight (g/mol) | 318.29 |  |
| Temp (K) | 100.0(2) |  |
| Crystal system | Trigonal |  |
| Space group | R-3 (no. 148) |  |
| a (Å) | 31.2520(16) |  |
| b (Å) | 31.2530(17) |  |
| c (Å) | 9.0913(5) |  |
| α (deg) | 90 |  |
| β (deg) | 90 |  |
| γ (deg) | 120 |  |
| V(Å3) | 7689.7(9) |  |
| Z | 18 |  |
| Dcalc(g/cm3) | 1.237 |  |
| μ(Cu Kα) (mm-1) | 1.554 |  |
| Nref, Nunique | 8177, 3429 |  |
| R1[I > 2σ(I)] |  | 0.0729 |
| wR2 (all data) | 0.2239 |  |
| CCDC number | 2093649 |  |

Figure S1. Results of TG/DSC analysis of mesityl(phenyl)phosphine oxide glycolate in the dynamic argon atmosphere 75 ml/min. Heating rate 10 °C/min.

Figure S2. Experimental diffractogram for mesityl(phenyl)phosphine oxide glycolate (blue curve), theoretical diffractogram calculated from data of single-crystal X-ray diffraction analysis of the compound mesityl(phenyl)phosphine oxide glycolate (red curve). For clarity, the curves are shifted relative to each other along the intensity axis.

Figure S3. View of crystal packing of 1 along the b axis showing voids.

Figure S4. Fragments of crystal packing of 1 showing intermolecular interactions with two neighbors (a) responsible for 35.0 kJ/mol (left neighbor), and 34.3 kJ/mol (right neighbor) as well as 18.3 kJ/mol interaction (b).

Figure S5. Hirshfield surface mapped dnorm along a, b and с axis (top) and Hirshfield surface mapped shape index along a, b and с axis (bottom).